ALS Laboratory Group

ANALYTICAL CHEMISTRY SERVICES

ALS Czech Republic, s r.o. Na Harfě 9/336, 190 00 Praha 9

Telephone: 	+420 284 081 646

Fax: 		+420 284 081 750

Internet: 	www.alsglobal.com, www.alsglobal.cz

E-mail: 		info@alsglobal.com

ENZYMIX s.r.o.

Frindova 612/24

407 46 Krásná Lípa

Test Report No. 21609 / 1 / 2007

In Prague: 29 October 2007

Project title: 		Analysis of samples regarding the content of metals

Date of sampling: 	Not specified

Samples received on: 	22 October 2007

Samples taken by: 	Client

Test performed on: 	22 - 29 October 2007

Test performed in: 	ALS Czech Republic, s.r.o. Na Harfě 336/9,190 00, Praha 9

Methods of determination, data on deviations, amendments or exemptions from testing regulations and other information:

Č-465735 	Q21-340-003/01 (CSN 46 5735, TNV 75 7440) Determination by means of Hg atomic absorption spectrometry.

I-1185		Q21-340-001/01 (EPA 200.7, ISO 11885) Determination of elements using the method of atomic emission spectrometry with inductively bound plasma: Ag, Al, As, B, Ba, Be, Ca, Cd, Co, Cr, Cr(VI), Cu, Fe, K, Li, Mg, Mn, Mo, Na, Ni, P, Pb, S Sb, Se, Sn, Sr, TI, V, Zn.

I-17294		Q21-340-002/01 (EPA 200.8, ČSN EN ISO 17294-2) Determination of elements using the method of mass spectrometry with  inductively bound plasma Ag, Al, As, B, Ba, Be, Cd, Co, Cr, Cr(VI), Cu, I, Li; Mg, Mn, Mo, Ni, Pb, Sb, Se, Sn, Sr, TI, V, Zn, Rh.

Q21-340-004/01	Sample treatment according to internal regulations.

Results of measurement

| Sample identification | Vermaktiv 1:200 | Vermaktiv 1:500 | Vermaktiv 1:1000 | unit | method |  |
| --- | --- | --- | --- | --- | --- | --- |
| Matrix | liquid for industrial use | liquid for industrial use | liquid for industrial use |  |  |  |
| Parameter | result nm | result nm | result nm |  |  |  |
| As | <0.0010 - | <0.0010 - | <0.0010 - | mg/l | I-17294 | A |
| Cd | <0.00050 - | <0.00050 - | <0.00050 - | mg/l | I-17294 | A |
| Cr | <0.0050 - | <0.0050 - | <0.0050 - | mg/l | I-11885 | A |
| Cu | <0.010 - | <0.010 - | <0.010 - | mg/l | I-11885 | A |
| Hg | <0.00030 - | <0.00030 - | <0.00030 - | mg/l | Č-465735 | A |
| Mo | <0.0010 - | <0.0010 - | <0.0010 - | mg/l | I-17294 | A |
| Ni | <0.0010 - | <0.0010 - | <0.0010 - | mg/l | I-17294 | A |
| Pb | <0.050 - | <0.050 - | <0.050 - | mg/l | I-11885 | A |
| Zn | <0.0050 - | <0.0050 - | <0.0050 - | mg/l | I-11885 | A |

The laboratory states that the test results included in this report apply only to the samples listed in this report and do not supersede any other documents. This report may only be copied in its entirety without written consent of the manager of the ALS ČR Laboratory.

seal: TESTING LABORATORY ACCREDITED BY ČIA (Czech Institute for Accrediation), ALS CZECH REPUBLIC, No. –1163-

signature illegible

Ing. Emilie Pokorná

Laboratory Manager Prague

Client: ENZYMIX s.r.o.							Test Report No. 21609/1/2007

Project: Analysis of samples regarding the content of metals			Date of sampling: not specified

Results of measurement

| Sample identification | Vermaktiv conc. | unit |  |  |
| --- | --- | --- | --- | --- |
| Matrix | solid for industrial use |  | method |
| Parameter | results nm |  |  |
| As | <0.10 - | mg/kg | I-17294 | A |
| Cd | <0.10 - | mg/kg | I-17294 | A |
| Cr | 0.21 ±20 | mg/kg | I-11885 | A |
| Cu | 1.1 ±20 | mg/kg | I-11885 | A |
| Hg | <0.10 - | mg/kg | Č.-465735 | A |
| Mo | <0.10 - | mg/kg | I-17294 | A |
| Ni | <0.10 - | mg/kg | I-17294 | A |
| Pb | <1.0 - | mg/kg | I-11885 | A |
| Zn | 5.1 ±20 | mg/kg | I-11885 | A |

Measurement uncertainty (NM [%]) is an extended uncertainty corresponding to 95% of the confidence interval. It is specified as an estimated relative standard deviation in per cent multiplied by the coefficient k = 2.

The parameters with 'A' index in the last column of the table are subject to accreditation, while the parameters with 'N' are not subject to accreditation.